2K Clears

HR-208 Super Gloss Clear

Product Description HR-208 Super gloss clear for application ranging from spot repair, panel repair to overall refinish.

Technical Characteristics Color: transparent Shelf life:24 months at 25°C Theoretical spreading rate:250-300 m2/l (avg) at 1 μm

Pre-treatment HR-208 super gloss clear is suitable to be applied on top of a clean and dust-free basecoat. See TDS of basecoat for other preparation of substrate.

| Further Treatment | HR-208 Clear 100(vol) 100 g HR-650 Hardener 50 (vol) 50 g HR-564T Thinner 20-25 (vol) 18-23 g Mix well and strain before application. Note: HR-650/HR-564F is for temperatures between 5°C–15°C HR-750/HR-564ST is for temperatures between 15°C – 25°C HR-850/HR-564S is for temperatures above 25°C HR-564EXS Thinner is for temperatures above 35° C or when refinishing large surfaces. 16 to 18 seconds DIN 4 cup at 25°C 3-4 hours at 25°C HVLP gravity-feed spraygun 1.2– 1.3 mm 1.5– 2.0 bar 10 – 15 cm Compliant gravity-feed spraygun 1.3 –1.6 mm 3.0– 4.0 bar 15 – 20 cm Number of spraycoats: 1thin + 1 wet coat Flash-off: 8 – 10 mins Film thickness: 40 – 50 μm Drying 25°C 60°C Dust free after 30-40 mins Ready for assembly after 6 hours 30 mins Ready for polish after 11-13 hours 60 mins IR drying after dust free Step 1 - short wave: 5 mins at a 80 cm distance Step 2 - medium wave: 20 mins at a 80 cm distance Polish after specified drying times and cooling. |
| --- | --- |